## Slide 1: Radiant Technologies, Inc. Ferroelectric Test & Technology
Joe T. Evans, Jr.
August 22, 2016

## Slide 2: Radiant Technologies
Focus on non-linear electromechanical materials technology. The company
  Designs and manufactures test instruments and their operating procedures
  Fabricates thin ferroelectric film devices
  Integrates the two disciplines to create unique functions.

## Slide 3: Test Instruments
Radiant pioneered ferroelectric test with the development of the first commercial test system in 1989 and now makes a variety of testers and fixtures.

## Slide 4: Test Instrument vs Integrated Ferroelectrics
What follows is a series of measurements demonstrating the properties of Radiant’s thin PZT capacitors measured with Radiant test equipment.

## Slide 5: IC Scale Cryogenic Testing
Lakeshore CRM-EM-HF

## Slide 6: IC Scale Cryogenic Testing
0.25m-thick PZT from 10 K to 310 K

## Slide 7: Quantum Design PPMS P450
The QD Model P450 Multifunction Probe can test disc-shaped bulk capacitors at high voltage down to 2.4 K.
B

## Slide 8
Bulk Capacitors vs Temperature
Many surprises await at lower temperatures.
The sample to the right is a commercial piezoelectric PZT from CTS Wireless in Albuquerque measured in a PPMS that indicates a normal hysteresis loop at room temperature but unexpectedly has no remanent polarization at 100 K.

## Slide 9: Leakage vs CV vs Remanent Polarization
Decomposing the hysteresis loop on a probe station.

## Slide 10: High Voltage Polarization & Piezeoelectric Loops
Bulk Capacitor displacement at high voltage and elevated temperature.

## Slide 11: Thin Film Polarization & Piezeoelectric Loops
The laser vibrometer can measure the piezoelectric motion of a thin ferroelectric film capacitor

## Slide 12
Thin Solid Capacitor Piezo Loop
AFMs work too. Surface piston of the 1µm-thick PNZT at 25 volts and 500 hertz using an AFM. The capacitor is clamped by the substrate.

## Slide 13
Thin Film PZT on Cantilever
Capturing e31 for a thin film on a cantilever surface is a 3rd technique.

## Slide 14
Ferroelectric Transistor Operation
PZT
InOx
Source & Drain
Gate

## Slide 15: Radiant Technologies
Integrated thin-ferroelectric-film capacitors.
  Radiant has developed a manufacturable process for discrete ferroelectric capacitors.
  Radiant inserts packaged capacitors into its testers as test references.
  Radiant processes thin PZT film wafers and devices for researchers studying non-linear materials.

## Slide 16: Membrane Capacitors
A three micron membrane with an embedded 1m-thick PNZT capacitor.

## Slide 17: Membrane Capacitors
Remanent strain movie if the same capacitor.

## Slide 18
pMEMs Devices
.
We have work still to do to reliably generate reproducible devices.

## Slide 19
Mechanically Coupled Capacitors
1.2mm
DRIVE
RETURN
GND
Sensor
Actuator
Actuator
Sensor
Actuator

## Slide 20
1 mm2 Membrane
A 1-square-millimeter capacitor with the majority of its surface as a membrane. In white light the membrane looks smooth but in Numarski the membrane is unmistakable.
White Light
Numarski

## Slide 21
16mm2 Membrane
A 16 square millimeter membrane soldered directly to a PCB with an on-board charge amplifier that connects to the Radiant EDU educational tester using telephone cable.
Pyroelectric constant is -22nC/cm2/K.
The membrane is too fragile to be touched by a human.

## Slide 22: Autonomous Analog Switch
This entire PCB with discrete components and a packaged ferroelectric capacitor can be shrunk into the same solid state switch package on the PCB in the left image. This circuit can stand-alone and resist disturbs from dramatic power-line voltage events.

## Slide 23
Nuts & Volts Magazine
“A Simple Ferroelectric Memory”
February 2015 Issue

## Slide 24
Ferroelectric Capacitor
Input Overvoltage
Protection
Output Buffer
Autonomous Memory
Event Input Line
Ferroelectric Circuits
Autonomous Event Detector

## Slide 25
Demo Board - Piezo
Piezo Flapper
Event Detector
Latch
This piezoelectric flapper is a Measurement Specialties, Inc. LDT0-28K Piezo Film Sensor. Bent 90 degrees, it generates exactly 7nC of charge, precisely the amount required to saturate one of Radiant’s Type AB 20/80 PZT or Type AD 3/20/80 PNZT thin film capacitors.
The Radiant ferroelectric capacitor is encased in the TO-18 transistor package on the Event Detector board.

## Slide 26
Magnetoelectric Sensor
Deposit magnetically sensitive material on membranes to make magnetic field sensors. Below are dice from a wafer prepared for this experiment but which have not yet seen the backside DRIE. This project, executed in a CRADA with SPAWAR, is difficult!

## Slide 27
Best Magnetoelectric Response
(so far)

## Slide 28
Autonomous Event Detector Set by a Magnetic Field?
Can we magnetomechanically switch the ferroelectric capacitor and control the switch?